## Slide 1
BASICS OF A GOOD ROAD ASPHALT AND AGGREGATES
Gerry Huber
Heritage Research Group

## Slide 4: Refinery Operation
FIELD STORAGE
PUMPING STATION
LIGHT DISTILLATE
HEAVY DISTILLATE
PROCESS
UNIT
ASPHALT
CEMENTS
FOR PROCESSING INTO
EMULSIFIED AND
CUTBACK ASPHALTS
STILL
AIR
AIR
BLOWN
ASPHALT
STORAGE
TOWER
DISTILLATION
REFINERY
RESIDUUM
OR
GAS
PETROLEUM
SAND AND WATER
CONDENSERS
AND
COOLERS
TUBE
HEATER
MEDIUM DISTILLATE
Notes: Distillation is used to separate the various crude fractions by boiling point ranges. The crude oil is heated in a large furnace to about 343 oC and partially vaporized. The remaining material is transferred to a distillation tower. Different fractions reach their boiling point ranges at various heights in the tower. When the temperature is reduced, each material condenses on a tray and is drawn off at each level.

## Slide 5: Not All Crude is the Same

## Slide 6
How Asphalt Behaves
Behavior Depends on
  Temperature
  Time of Loading

## Slide 7: Effect of Temperature

## Slide 8
How hard is the water?

## Slide 9: SUPERPAVE Asphalt Binder Specification
Grading System Based on Pavement Temperatures
(Summer) (Winter)
PG 64-22
Performance
Grade
Max pavement
design temp
Min pavement
design temp

## Slide 10: Asphalt Binder Tests
Temperature, C
- 20 20 60 135
Done at different temperatures

## Slide 11: Temperature Grades
High Temperature
  58
  64
  70
  76
Low Temperature
  -22
  -28
Rule of 90

## Slide 12: Temperature Grades
Unmodified Asphalt
  58-28
  64-22
Modified Asphalt
  64-28
  70-22
  70-28
  76-22
Rule of 90

## Slide 13: Base Grade
PG 64-22 or PG 58-28
PG 64-22

## Slide 14: Changing Base Grade
Bumping Grade
For heavy truck traffic, stopped condition
  Increase 2 high temperature grades
  64-22 to 76-22
Dropping Grade
For high RAP or Shingle use (+25% asphalt replacement)
  Decrease one high and low temperature grade
  64-22 to 58-28

## Slide 15: Aggregates

## Slide 16: Quarry

## Slide 17: Gravel Pit

## Slide 18: Aggregate Properties
Crushed Faces
Fine Aggregate Angularity
Gradation
Notes: Source aggregate properties are those properties which are measured for the aggregate as-stockpiled and are commonly used for aggregate source acceptance control. These properties are toughness, soundness, and deleterious materials. In addition, the gradations of individual stockpiles may be evaluated.

## Slide 19: Percent Crushed Particles
0% Crushed 100% with 2 or More
Crushed Faces
Aggregate shape influences
  strength
  compactability

## Slide 20: Coarse Aggregate Crushed Faces

## Slide 21: Fine Aggregate

## Slide 22: Fine Aggregate Angularity
Natural sands: typically 37 to 44
Manufactured sands: typically 42 to 52

## Slide 23: Fine Aggregate Angularity

## Slide 24: Gradation

## Slide 25: Washed Gradation

## Slide 26: INDOT Fine Aggregate Sizes

## Slide 27: INDOT Coarse Aggregate Sizes

## Slide 28
100
0
.075 .3 2.36 4.75 9.5 12.5 19.0 #200 #8 #4 3/8 1/2 3/4
Percent Passing
control point
max density line
max
size
nom
max
size
Sieve Size (mm) Raised to 0.45 Power
Primary control sieve

## Slide 29: Mix Size Designations
By Nominal Maximum Sieve
By Gradation
e.g. 12.5 mm, coarse graded
Sizes
  25.0 mm 1 in
  19.0 mm ¾ in
  12.5 mm ½ in
  9.5 mm 3/8 in
  4.75 mm #4
Coarse
Fine

## Slide 30: Hot Mix Gradation

## Slide 31: Asphalt Mix Design

## Slide 32: Asphalt Mixture Design
Superpave Mix Design
  Gyratory Compactor
Volumetric Properties
  Asphalt content for durability
  Air Voids
    Upper limit to control aging
    Lower limit for traffic densification

## Slide 33
Place pre-heated aggregate in bowl and add hot asphalt
Mixing
Notes: Pour the heated binder into a bowl with the heated aggregate. Typically the temperature for this is about 275 to 325 C.

## Slide 34: Mixing
Mix until aggregate is well-coated
Notes: The mixture is typically mixed in a mechanical mixer. The mix should be observed to insure that the aggregate and asphalt are thoroughly mixed.

## Slide 35: Short Term Aging
Simulate Construction
Oven Aging
  2 hours at 275°F

## Slide 36: Compaction
Place funnel on top of mold and place mix in mold.

## Slide 37: Compaction
Gyratory Compactor.

## Slide 38: Compaction
Gyratory compactor
  Shearing action
  150 mm (6 inch) diameter molds
    Aggregate size up to 1.5 inches
    Measure height during compaction
1.25o
Ram pressure
600 kPa
(90 psi)

## Slide 40
% binder
VMA
% binder
VFA
% binder
%Gmm at Nini
% binder
%Gmm at Nmax
% binder
DP
% binder
Va
Blend 3
Selection of Design Asphalt Binder Content
Notes: The properties are plotted verses the binder content and the proper AC content is obtained.