## Slide 1: An evaluation of in vitro and in vivo toxicity of chitosan-pDNA polyplexes
Kae Amaraporn
The Department of Pharmaceutics and Translational Therapeutics College of Pharmacy

## Slide 2: Gene delivery to lung
The transmission of DNA encoding for therapeutic gene or protein into the target cells for prevention or treatment of disease
Potential treatment for
  Cystic fibrosis, Asthma
Advantages
  Easily accessible via airways
  Large surface area for transfection
  Reduces the risk of systemic side effects
Disadvantages
  Repulsion between DNA & cell membrane due to same charge
  Enzymatic degradation
Mohammadi, Z., et al., In vivo transfection study of chitosan-DNA-FAP-B nanoparticles as a new non viral vector for gene delivery to the lung. Int J Pharm, 2011. 421(1): p. 183-8. Albelda, S.M., R. Wiewrodt, and J.B. Zuckerman, Gene therapy for lung disease: hype or hope? Ann Intern Med, 2000. 132(8): p. 649-60.
Notes: Gene therapies utilizing modified viruses or plasmid DNA (pDNA) to re-introduce functional copies of defective or mutated genes
are being investigated for the treatment of a wide range of lung diseases
CF is caused by the mutations in the gene encoding the Cystic Fibrosis Transmembrane Conductance Regulator protein (CFTR)
CF: transporting Cl- and Na+ across the epithelial membrane
CF: mucous build up, decrease mucocillary clearance and inflammation
Disadvantages for gene delivery to the lung
  Insufficient gene delivery
  Inflammatory response

## Slide 3: Cationic polymers:DNA complex
  Storrie, H. and D.J. Mooney, Sustained delivery of plasmid DNA from polymeric scaffolds for tissue engineering. Adv Drug Deliv Rev, 2006. 58(4): p. 500-14.
  Shan, Y., et al., Gene delivery using dendrimer-entrapped gold nanoparticles as nonviral vectors. Biomaterials, 2012. 33(10): p. 3025-35.
Notes: Advantages:
  condense DNA into a small particle, low immunogenicity, easy to manufacture
Disadvantages:
  Toxicity, low transfection effieicncy and lack of biodegradability and biocompatibility
Acidic endosome buffering (pH 7.4)
At lower pH, the buffering by PEI causes an influx of Cl- and H2O into endosomes which eventually burst out due to the osmotic pressure then facilitating intracellular release of the complex

## Slide 4: Bacterial plasmids
Bacterial plasmids are circular DNA which can replicated independently of the bacterial chromosome.
Bacterial DNA is rich in unmethylated CpGs
  activate the immune system
  induce inflammatory response (in vivo)
  decrease transgene expression
This study, we studied 2 types of pDNAs
  CpG(-) is a plasmid free of CpG
  CpG(+) is a plasmid containing CpG
www.qiagen.com
Notes: CpG: unmethylated 2’-deoxyribo (cytidine-phosphateguanosine)
The best nanoplex is high transfection efficiency, low toxicity, low or non-induced inflammatory response
Recently, there are studies shows that CpG motifs in plasmids are associated with…
   Transgene expression
  Induce inflammatory response (in vivo)

## Slide 5: Objectives
To characterized and optimized chitosan/pDNA polyplex formulations
  Size and charge
  Ability to condense plasmids
To investigate the toxicity and transfection efficiency in A549 and HEK293
  MTS assay
  Luciferase assay
To investigate the inflammatory response induced by the polyplexes in a mouse model

## Slide 6: Experiments and Results

## Slide 7: Objectives
To characterized and optimized chitosan/pDNA polyplex formulations
  Size and charge
  Ability to condense plasmids
To investigate the toxicity and transfection efficiency in A549 and HEK293
  MTS assay
  Luciferase assay
To investigate the inflammatory response induced by the polyplexes in a mouse model

## Slide 8: Preparation of the chitosan/pDNA polyplex
(+) charged polyelectrolyte was poured into (-) charged polyelectrolyte then vortexted for 20-30 s leading to the formation of the polyplexes
pDNA
Dextran
sulfate
30 min
Chitosan
in Acetate buffer
CH/DS-pDNA
nanoplex
*pDNA 50 ug/ml *CH:DS = 10:1 (w/w)
*Concentration of chitosan depends on N/P ratios

## Slide 9: Characterization
CH/CpG(-)
CH/CpG(+)
Size
Charge
Notes: - The nanoplexes were measured by Zetasizer Nano ZS in acetate buffer, pH 5.46, at 25C. Data expressed as mean ± SD (n=3).

## Slide 10: Gel Retardation Assay
1% Agarose gel contains ethidium bromide loaded with CH/CpG(+) polyplexes.
Chitosan can entrapped pDNA and inhibit DNA migration at N/P ratios > 1.
DNA ladder
pDNA
N/P 1
N/P 5
N/P 10
N/P 20
N/P 60
N/P 100
Notes: Condensation of DNA by chitosan

## Slide 11: Objectives
To characterized and optimized chitosan/pDNA polyplex formulations
  Size and charge
  Ability to condense plasmids
To investigate the toxicity and transfection efficiency in A549 and HEK293
  MTS assay
  Luciferase assay
To investigate the inflammatory response induced by the polyplexes in a mouse model

## Slide 12: Cell lines
A549
  Human lung carcinoma
www.atcc.org
HEK293
  Human embryonic kidney
Notes: A549 – adenocarcinomic human alveolar basal epithelial cells
  Squamous Adherent cells
  They grow as monolayer cells
HEK293

## Slide 13: Cationic polymers:DNA complex
  Storrie, H. and D.J. Mooney, Sustained delivery of plasmid DNA from polymeric scaffolds for tissue engineering. Adv Drug Deliv Rev, 2006. 58(4): p. 500-14.
  Shan, Y., et al., Gene delivery using dendrimer-entrapped gold nanoparticles as nonviral vectors. Biomaterials, 2012. 33(10): p. 3025-35.
Notes: Advantages:
  condense DNA into a small particle, low immunogenicity, easy to manufacture
Disadvantages:
  Toxicity, low transfection effieicncy and lack of biodegradability and biocompatibility
Acidic endosome buffering (pH 7.4)
At lower pH, the buffering by PEI causes an influx of Cl- and H2O into endosomes which eventually burst out due to the osmotic pressure then facilitating intracellular release of the complex

## Slide 14: Transfection efficiency
Firefly luciferase activity assay
  Firefly luciferase is
    61kDa protein – cosubstrate to catalyzes luciferin oxidation
    sensitive assay to study gene expression
www.promega.com
Notes: Firefly luciferase: good reporter to study gene expression because
  The reporter activity is available immediately upon the translation since the protein does not require post translational processing
  The protein does not require post translational procession
  The assay is very sensitive because its light production has the highest quantum effiency known for any chemiluminescent reaction and no background luminescence is found in the host cells or the assay chemistry
  The assay is rapid requiring only a few seconds per sample
luciferin + ATP → luciferyl adenylate + PPi
luciferyl adenylate + O2 → oxyluciferin + AMP + light
Translation: Wikipedia
  The third stage of protein biosynthesis (part of the overall process of gene expression).
  mRNA produced by transcription is decoded by the ribosome to produce a specific amino acid chain which will later fold into an active protein.
  In bacteria, the translation occurs in the cell’s cytoplasm.
  In eukaryotes, it occurs across the membrane of endoplasmic reticulum. (tRNA)
  Initiation, elongation, translocation and terminition

## Slide 15: Transfection experiment
24-well plate
1 day
48 h
4 h
0 h
CH/pDNA
PBS and RLB
24 h
Luciferase assay and Micro BCA assay
Notes: A549 and HEK293, 24-well plate cell density 8X104 cells/well 24 h prior transfection
0h: + CH/pDNA (N/P 1-100) (100 µl)
(pDNA 5 µg/well) + serum free media (500 µl)
4h: + fresh complete media
24h: replaced media with fresh complete media
48h: removed media, wash with PBS + RLB 2xfreeze-thaw cycles centrifuged at 13200rpm, 5 mins
Luciferase assay (Promega) (RLU value)
Micro BCA assay (Pierce) (mg of protein)

## Slide 16: Luciferase expression
CH/CpG(-)
CH/CpG(+)

## Slide 17: Luciferase expression
CH/pCpG-Luc
CH/VR1255
pCpG-Luc: CpG-free plasmids
VR1255: plasmids contain CpG

## Slide 18: MTS assay
MTS is bioreduced by cells into formazan (color).
The quantity of formazan production is proportional to number of living cells.
www.promega.com
Notes: This conversion is from NADPH or NADH produced by dehydrogenase in metabolically active cells.

## Slide 19: MTS assay
96-well plate
1 day
48 h
4 h
0 h
CH/pDNA
MTS reagent
Notes: A549 and HEK293, 96-well plate cell density 1X104 cells/well 24 h prior
0h: + CH/pDNA (N/P 1-100)
(pDNA 1 µg/well) + serum free media
4h: + fresh complete media
48h: replaced media with 100 µl fresh complete media + 20 µl of CellTiter 96® Aqueous One solution (Promega)
incubate at 37° for 1-4h in a humidified, 5% CO2
Measured the absorbance at 490 nm

## Slide 20: Cytotoxicity assay: MTS
CH/CpG(-)
CH/CpG(+)
CH/CpG(-)
CH/CpG(+)

## Slide 21: MTS assay (vary conc)
A549 96-well plate cell density 104 cells/well 24 h prior
0h: + CH/pDNA (N/P 1-100)
(pDNA 1-33 µg/well) 120 µl + serum free media
4h: + fresh complete media
48h: replaced media with 100 µl fresh complete media + 20 µl of CellTiter 96® Aqueous One solution (Promega)
incubate at 37° for 1-4h in a humidified, 5% CO2
Measured the absorbance at 490 nm
pCpG-Luc: CpG-free plasmids
VR1255: plasmids contain CpG

## Slide 22: MTS assay
Increasing Chitosan N/P ratio = Reducing % relative cell viability
Compare with PEI/pDNA, Chitosan/DS-pDNA nanoplexes still consider less toxic in every N/P ratio.
At CH/pCpG-Luc N/P 10 (33 µg pDNA/well): 51.26%
pCpG-Luc: CpG-free plasmids
VR1255: regular plasmids

## Slide 23: Objectives
To characterized and optimized chitosan/pDNA polyplex formulations
  Size and charge
  Ability to condense plasmids
To investigate the toxicity and transfection efficiency in A549 and HEK293
  MTS assay
  Luciferase assay
To investigate the inflammatory response induced by the polyplexes in a mouse model

## Slide 24: In vivo study
CH/pDNA polyplexes
CH/pDNA polyplexes
1 h
24 h
BAL
fluid
C57Bl/6 (n=6)
Supernatant from homogenized lung
Luciferase assay
Micro BCA assay
Total cell count
Total protein/LDH
Cytokines

## Slide 25: Luciferase expression in mice lungs
Mice treated with CH/CpG(-) shows highest luciferase expression.

## Slide 26: Number of cells in BAL fluids
Mice treated with CH/CpG(-) shows maximum number of total cell count in BAL fluids.
Among three types of white blood cells, BAL fluids contain high neutrophils in both types of polyplexes.

## Slide 27: Total protein and LDH activity

## Slide 28: Cytokines
IL-6
IL-12
KC
MIP-1α
TNF-α

## Slide 29: Conclusion
Characteristic of Chitosan/pDNA polyplex
  size  100-170 r.nm
  charge  20-30 mV
CH/pDNA polyplex shows low cytoxicity in A549 and HEK293. There is no difference in toxicity between the nanoplex created using CpG(-) or CpG(+).
The polyplex prepared from from CpG-free plasmids shows …
  higher transgene expression in A549 and in mice lungs
  less inflammation in vivo
N/P ratio and DNA content of Chitosan/pDNA polyplex plays an important role in achieving high gene expression with minimal toxicity and inflammation.

## Slide 30: Future work
To study lung histopathology of mice when treated with the chitosan/pDNA polyplex
  Lung abnormalities
  Abnormal inflammatory infiltrates
To develop chitosan/pDNA polyplex formulation which can form complex at high concentration and give high transfection efficiency
To investigate the difference between nasal instillation and aerosol delivery