## Slide 1: RESIN TRANSFER MOLDING (RTM)

## Slide 2: RTM PROCESS
impregnating preformed dry reinforcement in a closed mold with wet thermosetting resin under pressure
production rate comparison
  2 - 8 pph (parts per hour)
  spray-up @ 0.5 pph
  SMC, injection molding @ 30 pph (chopped fibers, high pressures requires >>$ tooling)

## Slide 3: REINFORCEMENTS USED IN RTM
type
  E-glass, S-glass
  carbon/graphite
  aramid
form
  mat
  fabric
  textile preform architecture (knitted, braided, 3-D stitched)
preforms - preshaping of reinforcement

## Slide 4: DESIGN OF PREFORMS
compression of fiber preform into the mold (denser the fiber, the more resistance it offers to impregnation by resin)
fiber orientation (resin flows faster along the length of the fiber than across it)
multiple layers or plies (impede or complicate the resin distribution)

## Slide 5: RESINS USED IN RTM
polyester, vinyl ester, epoxy
desired resin characteristics
  must remain liquid as it is held in the reservoir prior to injection
  must impregnate fiber preform quickly and uniformly without voids
  must gel as quickly as possible once impregnation occurs (fast cycle time)
  must possess sufficient hardness to be demolded without distortion
low viscosity critical (< 1,000 cps to impregnate preform loading of 50%)
low viscosity resin requires less pressure to achieve adequate wet-out
injection temp (typically elevated) of resin should be held as close as possible to minimum viscosity to insure preform impregnation, yet higher temp accelerates cure, cutting into injection time

## Slide 6: RTM EQUIPMENT
resin/curing agent (catalyst) mixing equipment
  positive displacement piston pumping cycle
  maintain accurate ratio control between resin and curing agent
  RTM process requires low injection pressures (30 psi - 100 psi)
  piston type positive displacement pumps are critical due to changing back pressure conditions - as resin is pushed through reinforcement an increasing back pressure builds against metering pumps - if slippage occurs at pump, resin/curing agent ratio will be affected
with resin system components accurately metered, sent through flexible hoses to a mix head

## Slide 7: THE MIX HEAD USES A MOTIONLESS MIXER
thoroughly blends resin and curing agents together immediately prior to injection
motionless mixers
  low volume curing agent injected into center of resin stream to assure complete and uniform mixing
  motionless mixers available in various diameters and lengths to suit a variety of resin viscosities and fillers

## Slide 8: MAY BE NECESSARY TO CONTROL RESIN TEMPERATURE THROUGHOUT RTM PROCESS
preheat resin (system) in reservoir, then maintain temp throughout process, using heating elements in material containers, the pumping mechanism, and the tool
recirculate the material continuously through the pumping mechanism and back to the reservoir during non-pumping segment

## Slide 9: MOLD DESIGN
gasket around perimeter
inlet injection port
  located at the lowest point of mold
  plug or check valve incorporated
vent ports located at highest point of mold
for high volume, tightly toleranced parts may use press - controls parallelism of mold set during opening and closing and holds mold closed during injection (alternative is manually clamping or fastening)

## Slide 10: RTM PROCESS
may or may not take place under vacuum (assists in minimizing air entrapment)
mixer/injection head is inserted into mold
injection pressure pushes check valve off its seat and allows resin to begin filling
air is pushed ahead of resin
resin will begin flowing from vent ports
  if part design is simple may be full
  if part design complex, may require slight overfill to vent all air
vent ports are pinched off and internal pressure causes inlet check valve to close

## Slide 11: RTM PROCESS ISSUES
critical to control infusion rate and flow front of resin so that it infiltrates fiber preform evenly and completely, but quickly before gelling
resin is injected in center of part to guard against formation of air pockets and minimize distance resin must travel
care must be exercised to insure reinforcement does not move during injection (fiber wash)

## Slide 12: ADVANTAGES OF RTM PROCESS
closed mold process
  lower emissions
  both sides of part have tool surface finish and/or can be gel coated
no air entrapment if properly designed (tooling, preform, and resin)
once process established very repeatable and predictable
permits relatively high fiber volume (40% - 50%)
preform design can incorporate damage tolerant features
close dimensional tolerances can be maintained (given proper clamping and mold closure)
significant part consolidation - ability to incorporate cores, ribs, and inserts
low tooling cost/short tooling lead times
versatile - prototype or high production rate (tooling)

## Slide 13: DISADVANTAGES OF RTM PROCESS
preform process
  preparation can be labor intensive
  process waste may be high
  because preform lacks strength may have to be assembled in mold (tying up mold)
preforms may be oversized in order to protrude from tool edge to provide escape route for displaced air and excess resin
oversized preforms will have to be trimmed (sealing or close-out will be required over exposed reinforcement to prevent potential path for moisture ingress)
movement of reinforcement during injection (fiber wash)
control of resin uniformity difficult - radii and edges tend to be resin rich
higher speed versions of process undeveloped - still problems filling large parts with high reinforcement content at low pressure
as part consolidation increases
  high losses for manufacturer if part scrapped
  replacement cost to consumer can be significant

## Slide 14: RELATED PROCESSES
RTM Light (YouTube video)
Infusion (YouTube video)