## Slide 1: MODIFICATION OF CELLULOSE BY ANIONIC POLYSACCHARIDES
UTTAM C. PAUL , A. P. Manian, B. Široká, T. Bechtold
Research Institute of Textile Chemistry and Textile Physics
University of Innsbruck, Austria
STEP-ITN Mid-year meeting, Dornbirn, Austria, 13-14 March 2012

## Slide 2
Outline of the Presentation
Introduction
Part 1: Ca2+ Modulated Interactions of Polysaccharides with Cellulose
Part 2: Sorption of Iron (III) and Alginate to cellulose from Iron (III)-Alginate Complexes
Part 3: Modification of Cellulose Fabric by Iron (III)-Polysaccharide Complexes
Potential Applications and Future Aspect of Work

## Slide 3
Cellulose
Alginate
Polysaccharides for cellulose modification
But,
cellulose is anionic and,
it is poorly compatible with another anionic polysaccharide matrix.
-Challenges of the research – incorporation of anionic polysaccharide, bring
novel functionalities, without deteriorating its strength properties
Introduction
Incorporation of polysaccharide to cellulose is an important field of research
-In textiles polysaccharides like alginate use as a sizing agent, print past and thickener. Deleterious effect!
Extensive chemical modifications!

## Slide 4
PART 1 Ca2+ Modulated Interactions of Polysaccharides with Cellulose

## Slide 5
DM Cellulose Fibers
Scheme : Sorption of polysaccharide into Ca2+ containing cellulose fibres
Pectin Molecules
Ca2+ ions
Ca2+
R. Kohn/PAC/1975, V.42, Issue 3, P 371-397
Immerse in Ca2+
Ca2+ Adsorbed Cellulose fibres
Immerse in PS
Ca2+- PS Adsorbed Cellulose Fibres

## Slide 6
Introduction Part 1
Paul, U.C., et al., Carbohydrate Polymers. 2012. 87. p. 695-700

## Slide 7
ESEM analysis of polysaccharides adsorbed fibres
Untreated Viscose (CV)
8mM Ca2+ -Pectin Treated CV
calculated thickness layer 7 nm

## Slide 8
Staining of Ca2+ by Alizarin Dye
DM CV
8 mM Ca2+ CV
Pectin CV
8 mM Ca2+, Pectin CV
Staining of Polysaccharides by Ruthenium Red Dye
Introduction Part 1 Part 2 Part 3 Applications

## Slide 9
PART 2 Sorption of Iron (III) and Alginate to Cellulose from Iron (III)- Alginate Complexes
Introduction Part 1 Part 2 Part 3 Applications

## Slide 10
Residual Alginate in exhausted solution
Cellulose Fiber
(CLY)
Immerse in
Fe (III) – Alginate Solution,
24 h, 300C and 600C
Fe (III) - Alginate -
Cellulose Fiber
Fe (III) content in fiber
Alginate content in fiber
Residual [Fe3+] in exhausted solution
Preparation of Fe (III) – Alginate
Complex Solution
0.5:1 M and 0.05:1 M, pH 3, 7, 9, 11, 13
Alginate and Fe (III) in blank solution
Experimental Procedure
FTIR
ESEM, K/S
Fiber Tenacity, Elongation and Abrasion resistance

## Slide 11
Sorption mechanism of Fe3+, alginate and cellulose
Bechtold, T., et al., Carbohydrate Polymers. doi. 10.1016/j.carbpol.2012.01.064

## Slide 13
Untreated Lyocell (CLY)
0.5: 1 M Fe3+-alginate Treated CLY
ESEM analysis of alginate adsorbed fibres
Calculated max. thickness layer of alginate is 22 nm

## Slide 14
PART 3 Modification of Cellulose Fabric by Iron (III)- Polysaccharide Complexes
Introduction Part 1 Part 2 Part 3 Applications

## Slide 15
Fe + Alginate complex
Add Fe(NO3)3 to sodium alginate
Add NaOH dropwise to Fe-Alginate mixture
All the above under stirring of ca. 1200 rpm –
continue stirring until homogeneous
solution formed
Final composition of complex:
    Fe: 0.02 mol/l
    Alginate: 0.04 mol/l
    NaOH: 0. 1 mol/l
Complex pH ≈ 12.7 Treatment Process: Pad batch Process
Fabric (viscose, woven)
Demineralized with EDTA at RT for 1 h – wash with DI water
(to remove Ca2+)
(a) Alginate , (b) (Fe + alginate) complex solution

## Slide 18
Introduction Part 1 Part 2 Part 3 Applications

## Slide 19
Untreated CV fabric
(Fe + alginate) complex treated CV fabric
ESEM analysis of (Fe + alginate) adsorbed fabric

## Slide 20
Ultraviolet Protection Factor (UPF)
AS/NZS 4399 Australian/New Zealand Standard®
Sun protective clothing—Evaluation and classification
UPF Rating | Protection Category | % UV Radiation Blocked
UPF 15 - 24 | Good | 93.3 - 95.9
UPF 25 - 39 | Very Good | 96.0 - 97.4
UPF 40 – 49, 50+ | Excellent | 97.5 or more

## Slide 21
Applications and Future Potential
Introduction Part 1 Part 2 Part 3 Applications
There is a growing interest for sustainable PS modified
fibers in different fields: textiles, pharmacuticals, and
reinforcement materials industry.
Applications:
Smart fabric
Sanitary goods
Smart dressing and wound healing
Color textiles (exellent color fastness properties)
UV protective textiles
The process is environmental friendly, so,
It is believe that this modification procedure can be used for
practical applications

## Slide 22
Thank you for your attention
The research leading to these results has received funding from the European Community’s Seventh Framework Programme [FP7/2007-2013] under Grant Agreement No. 214015.

## Slide 23
Untreated CV
(Fe + alginate) complex treated CV
Light micrographs of
(Fe + alginate) complex
treated CV

## Slide 24
T = thickness of polysaccharide layer (nm),
d = fiber linear density (1.3 dtex = 1.3 g/10,000 m),
r = fiber radius (m), P = average polysaccharide content on fiber (g/g),
 = polysaccharide density (approximated at 1 g/cm3).

## Slide 25
UPF after Ruthenium Red Dye