## Slide 1: Rubberized Asphalt Pavement
Waste Tire Working Group
Department for Environmental Protection
Energy and Environment Cabinet
December 3, 2013
Notes: I-35 San Antonio TX RPA

## Slide 2: Rubberized Asphalt Pavements
Topics
  Why Rubberized Asphalt?
  Common Questions & Answers
  Possible Kentucky Uses
  Pilot Project
  Where do we go from here?
  Resources
Notes: Specs written without much thought.
Trial-and-error projects commenced
Was to be the primary scrap tire market in U.S.

## Slide 3: Why Rubberized Asphalt?
  Tire Derived Fuel $20-40/ton
Notes: Specs written without much thought.
Trial-and-error projects commenced
Was to be the primary scrap tire market in U.S.

## Slide 4: Why Rubberized Asphalt?
Crumb rubber $200-400/ton
Notes: Specs written without much thought.
Trial-and-error projects commenced
Was to be the primary scrap tire market in U.S.

## Slide 5: Rubberized Asphalt Pavements
  81% Waste Tires Recycled in KY
    18% still landfilled
Notes: Specs tried & true
Evaluate based on engineering properties

## Slide 6: U. S. Markets or Tests

## Slide 7: Binder and Pavement Rehabilitation
Stress Absorbing Membrane Interlayer (SAMI)
  SAM with Rubberized Gap Graded Asphalt overlying layer
Before: San Jose, p. 4 Western Pavement Maintenance Forum
2009 Award of Excellence in Contracting Chip Seal / Innovation Category

## Slide 8: Binder and Pavement Rehabilitation
After: San Jose, p. 5 Western Pavement Maintenance Forum
2009 Award of Excellence in Contracting Chip Seal / Innovation Category

## Slide 9: Binder and Pavement Rehabilitation
TWO AND THREE LAYER SYSTEMS
  Asphalt-rubber SAMI and either the gap or open graded hot mix material as the final wearing course
  Avoids costly reconstruction

## Slide 10: Frequently Asked Questions
How many waste tires can be used?
  A two-inch-thick RAC resurfacing project uses about 2,000 scrap tires per lane mile (CAL Recycle)
  Depending on type of use, 500-2,000 tires per lane-mile (Liberty Tire)

## Slide 11: Frequently Asked Questions
How many waste tires are used?
  rubberized asphalt uses 100 million pounds of crumb rubber per year (RMA Market Report for 2007).
    2% U.S. Waste Tire Generation
    FL highest with 5% of annual
    waste tire generation

## Slide 12: Frequently Asked Questions
Why isn’t it more widely used?
  “Experimental”
  Engineers expected comfort with the usual materials
    Test sections needed to familiarize engineers, contractors, plant operators
    Training of asphalt plant hot mix operators by AR operators is required

## Slide 13: Frequently Asked Questions
Does the use of rubber cause dangerous emissions?
  New additives reduce emissions
  NIOSH finds emissions no more generally than conventional asphalt
  Aroma is different

## Slide 14: Frequently Asked Questions
Can rubberized asphalt be recycled?
  City of Los Angeles. LA., recycled a 12-year old RA pavement
  Met specifications and passed all tests

## Slide 15: Frequently Asked Questions
Can RA be used in cold climates?
  California uses in Sierra Mountains
  Alaska and Sweden use to counter snow tires stud damage
  Massachusetts and New Jersey use
  Proper mix design and construction practices are critical (no OGFC)

## Slide 16: Possible Uses in KY
Polymer Replacement
  Polymer shortage increased cost in 2008 and changed projects
  KY TC paved interstates using PG specs without polymer
  Rutting susceptibility potential increased and pavement endurance decreased
  TC wants to be in a position to continue paving should polymer shortage return

## Slide 17: Pilot Project
To Protect and Enhance Kentucky’s Environment
TAG Resource Recovery
Eaton Asphalt Paving Co.
Modified Asphalt Solutions, Inc

## Slide 18: Pilot Project
July 24, 2013 Planning Meet at District 6, Florence:
  Rejected KY 18 (Road to Florence Mall from I-75) due to structural problems with underlying concrete
  Selected KY 8 (2.2 mile from I-471 to Dayton KY)

## Slide 19: Pilot Project
July 24, 2013 Planning Meet at District 6, Florence:
  One lane is control using standard asphalt and 0.38A PG 76-22 (interstate grade) Superpave 0.38 spec.
  Both 6.0% base asphalt, 5.0-5.2% liquid with 20% RAP
  Other lane is same as above plus 14% ground tire rubber with 100% passing #30 size

## Slide 20: Pilot Project
July 24, 2013 Planning Meet at District 6, Florence:
  EEC to pay $85,000 over initial $651,000 project costs
    $70,000 to TC for rubberized asphalt and interstate quality asphalt over regular street asphalt
    $15,000 to UK for long-term testing

## Slide 21: Pilot Project
September 25, 2013 Preconstruction Meet and Project Start:
  Discussed testing
  Ingredient added to make rubberized asphalt handle similar to regular asphalt, decreases rubber smell

## Slide 22: Pilot Project
  Spraying the tack coat looking northeast. Ohio River floodwall on right and background. Photo by Mark Belshe RPA

## Slide 23: Pilot Project
  Paving train applying rubberized asphalt looking west. Photo by Mark Belshe RPA

## Slide 24: Pilot Project
  Paving train applying rubberized asphalt looking southwest. Photo by Mark Belshe RPA

## Slide 25: Pilot Project
  Workers smoothing rubberized asphalt around manholes looking southwest. Photo by Mark Belshe RPA

## Slide 26: Pilot Project
  Vibratory roller with view to southeast.
  Photo by Mark Belshe RPA

## Slide 27: Pilot Project
  Downtown Dayton KY rubberized and polymer asphalt. Photo by Brian Donnelly TC

## Slide 28: Pilot Project
  Close-Up of control and rubberized asphalt. Photo by Brian Donnelly TC.

## Slide 29: Pilot Project
  Close-up of rubberized asphalt. Photo by Brian Donnelly TC.

## Slide 30: Pilot Project Results
Density Tests: 100% payment or 92% density
Initially there were high void content in the mix, but this was quickly brought under control with deletion of sand and add 0.3% asphalt.

## Slide 31: Pilot Project Results
Constant adjustments made at plant
  District 6 QA suspects rubber settlement occurred
  Contractor says 14% AR too high
  Rubber particles meet spec (100% passing #30 sieve)
  RPA engineer says worked like regular asphalt
  FL DOT says watch settling of rubber particles (stir, haul distance)

## Slide 32: KTC Pilot Project Results
KY Transportation Center permeability tests yield normal results
Spring: Skid testing, visual survey, another round of cores

## Slide 33: Pilot Lessons Learned
Look at lower AR% used by other states: FL 10%, GA 5%
  May require +polymer or additive
  May require KY to lower elasticity spec from 75% to 70% or lower (KY highest in U.S.)

## Slide 34: Pilot Lessons Learned
Do another pilot project that meets 70-22 GTR spec and do long-term testing (contractor)
Not many contractors in state have vertical tanks or stirring equipment like Eaton
KY not ready if polymer prices increase

## Slide 35: Pilot lessons Learned
Rubberized Asphalt currently costs $12.00 per ton vs. $8.00 polymer-modified asphalt
  Costs good only for this project
  Costs varies with transportation distance and other factors
  May swing the other direction with polymer shortage

## Slide 36: After Pilot
KTC & DWM attended Rubberized Asphalt Conference in AZ Oct. 14-17, 2013
DWM led round table at KACo annual meeting November 21
Presentation to Annual Meeting for Plantmix Asphalt Industry of Kentucky in February 2014 at Louisville

## Slide 37: After Pilot
Plot polymer shortage strategy with Division of Materials to adjust specs , tests or recommendations
Pursue future hot-mix pilot with Transportation Cabinet
Pursue chip-seal pilots with counties

## Slide 38: Resources

## Slide 39: Resources

## Slide 40: Resources
http://rubberpavements.org/
http://www.ra-foundation.org/

## Slide 41: Resoruces
http://www.rma.org/scrap-tires/
Notes: For scrap tires, Divert 85% of newly generated scrap tires to reuse, recycling or energy recovery by 2008 (vs. 70% in 2003)
The goal of the RCC is to achieve a 35% US Recycling rate by 2008 (with 2003 as a baseline).
I am Vice-Chair of the U.S. EPA RCC Scrap tire TDF committee. It is made up of federal, state and industry professionals. Mike Giuranna of U.S. EPA, Region III is the chairman.

## Slide 42: Resources
U.S. EPA
Scrap Tire Workgroup Website
http://www.epa.gov/wastes/conserve/materials/tires/workgroup.htm
Notes: For scrap tires, Divert 85% of newly generated scrap tires to reuse, recycling or energy recovery by 2008 (vs. 70% in 2003)
The goal of the RCC is to achieve a 35% US Recycling rate by 2008 (with 2003 as a baseline).
I am Vice-Chair of the U.S. EPA RCC Scrap tire TDF committee. It is made up of federal, state and industry professionals. Mike Giuranna of U.S. EPA, Region III is the chairman.

## Slide 43: Questions?
George Gilbert, P.E.
Environmental Engineer Consultant
Director’s Office
KY Division of Waste Management
george.gilbert@ky.gov
(502) 564-6716
Member U.S. EPA Scrap Tire Committee
To Protect and Enhance Kentucky’s Environment